## Slide 1
PHOTOELASTIC PROPERTIES OF K2SO4 DOPED WITH COPPER
Pavlo Shchepanskyi
ISPCS'20 – 17.06.2020
V. Y. Stadnyk1, R. B. Matviiv1, R.S. Brezvin1, P.A. Shchepanskyi1,2
1 Ivan Franko National University of Lviv, Dragomanova St., 19, 79005 Lviv, Ukraine
e-mail: vasylstadnyk@ukr.net
2 Jan Dlugosz University in Częstochowa, Al. Armii Krajowej 13/15, 42-200 Czestochowa, Poland

## Slide 2
K2SO4
orthorombic
Pnma
hexagonal
P63/mmc
860 K
K2SO4
K2SO4:Cu2+ (1,7 %, 3 %)
AВSO4 system
A is the alkali-metal ion
B is alkali-metal ion or NH4 group
K2SO4, LiKSO4, Li2SO4, RbNH4SO4, LiNH4SO4

## Slide 3
XRPD of K1.84(1)Cu0.08(1)SO4 compound
Crystal structure
Atom | Wyckoff position | x | y | z | Biso, Å2 | G
K1 | 4c | 0.1727(3) | 1/4 | 0.4112(3) | 1.45(8) | 0.939(4)
K2 | 4c | 0.4894(3) | 1/4 | 0.7020(2) | 0.90(7) | 0.903(4)
S | 4c | 0.2308(3) | 1/4 | 0.0804(3) | 1.70(9) | 1
O1 | 4c | 0.0351(7) | 1/4 | 0.0818(6) | 2.1(2) | 1
O2 | 4c | 0.7927(9) | 1/4 | 0.5626(6) | 2.0(3) | 1
O3 | 8d | 0.3011(6) | 0.0363(7) | 0.1472(4) | 1.7(2) | 1
Cu | 8d | 0.110(7) | 0.083(3) | 0.257(5) | 1.8(2) | 0.040(2)
Fig. 1.

## Slide 4
Crystal structure
Fig. 2. Stacking of metal component atoms and SO4 tetrahedra in the structure of K2SO4:Cu2+ crystals
Fig. 3. Second oordination environment of the anionic
group in the structure of K2SO4:Cu2+ crystals.
Fig. 4. Coordination environment and interatomic distances of Me-O in the structure of K2SO4:Cu2+ crystals.

## Slide 5
Refractive parameters
 | Bi, 10-6 nm-2 | Bi′, 10-9 nm-2 | λ0i, nm | Ri,10-6 m3 | αi, 10-24 cm3
X (pure) | 148.033 | 6.738 | 90.322 | 19.217 | 7.622
X (Cu wt 1.7%) | 142.961 | 4.610 | 91.734 | 19.185 | 7.609
X (Cu wt 3%) | 135.432 | 2.195 | 94.046 | 19.158 | 7.599
Y (pure) | 147.527 | 6.137 | 90.329 | 19.164 | 7.601
Y (Cu wt 1.7%) | 142.757 | 3.742 | 91.673 | 19.144 | 7.593
Y (Cu wt 3%) | 134.921 | 1.504 | 94.096 | 19.125 | 7,586
Z (pure) | 146.175 | 4.576 | 91.130 | 19.295 | 7.653
Z (Cu wt 1.7%) | 140.231 | 2.217 | 92.859 | 19.269 | 7.643
Z (Cu wt 3%) | 134.597 | 0.608 | 94.657 | 19.263 | 7.640
 | a, Å | b, Å | c, Å | V, Å3 | density ρ, g/cm3
pure | 7.4776 | 5.7704 | 10.0712 | 434.56 | 2.66
Cu wt 1.7% | 7.4773 | 5.7716 | 10.0738 | 434.74 | 2.649
Cu wt 3.0% | 7.4777 | 5.7717 | 10.0735 | 434.76 | 2.641
 | n1 | n2 | n3 | n4 | n5 | n6
Pure crystal | 1.4959 | 1.4922 | 1.4934 | 1.4928 | 1.4946 | 1.4940
Cu wt = 1.7% | 1.4950 | 1.4913 | 1.4924 | 1.4918 | 1.4937 | 1.4931
Cu wt = 3.0% | 1.4944 | 1.4902 | 1.4913 | 1.4907 | 1.4928 | 1.4923

## Slide 6
Piezo-optical coefficients
Spectral dependences of the combined piezo-optical constants of K2SO4 (Cu wt 3%) crystals at room temperature : 1 – π120; 2 – π230; 3 – π310; 4 – π210; 5 – π320; 6 – π130
1

## Slide 7
Piezo-optical coefficients
 | π11 | π12 | π13 | π21 | π22 | π23 | π31 | π32 | π33 | π44 | π55 | π66
1,7 % | 2.1 | 2.7 | 0.7 | –0.8 | 1.0 | –1.8 | 2.0 | 3.2 | 2.6 | 7.3 | 1.8 | –2.6
3,0 % | 2.0 | 2.6 | 0.7 | –0.7 | 1.0 | –1.7 | 2.0 | 3.1 | 2.5 | 7.3 | 1.7 | –2.4
 | р11 | р12 | р13 | р21 | р22 | р23 | р31 | р32 | р33 | р44 | р55 | р66
1,7 % | 0.13 | 0.21 | 0.13 | 0.05 | 0.17 | 0.04 | 0.22 | 0.28 | 0.15 | 0.02 | 0.03 | –0.07
3,0 % | 0.12 | 0.20 | 0.11 | 0.04 | 0.15 | 0.03 | 0.20 | 0.26 | 0.14 | 0.01 | 0.02 | –0.06
Rotational–shift components
рin = πimCmn,
p11 = π11 С11 + π12 С12 + π13 С13,
p12 = π 11 С12 + π12 С22 + π13 С32,
p13 = π 11 С13 + π12 С23 + π13 С33,
p44 = π44 С44
3
4
5
6
7
2
Pockels relations ni3ii – nj3ji = 2(im0m – s12(nj – ni)m) (i, j, k = 1, 2, 3)

## Slide 8
ρ = 2660 kg/m3
max(pi) = р32 n3 = 1.4934
Cijklmjmk = ρV 2gl
Cijkl – the components of the elastic stiffness tensor; mj, mk are the unit vector components of the wave normal component; gl are the unit vector components of the transversal wave
V2 = 4292 m/s.
Acoustooptical efficiency
М2 = 4.8×10–15 s3/kg.
8
9

## Slide 9
The spectral dependences of the absolute piezooptic constants are calculated using the experimentally obtained spectral dependences of the birefringence of Cu-doped potassium sulfate crystals under the action of uniaxial stresses
The matrix of elastooptic coefficients pin of these crystals is filled using the values of elastic stiffness coefficients and absolute piezooptic coefficients
The elastooptical effect as well as the piezooptical effect is quite noticeable in doped potassium sulfate crystals
The highest values of the pin coefficients are at the range from 0.20 to 0.30.
The maximum values of the acoustooptical coefficient of Cu-doped potassium sulfate crystals are nearly an order of magnitude higher than that of quartz and strontium borate, which are suitable for AO light modulation at the ultraviolet spectral range
Conclusions

## Slide 10
Thank you for attention!