## Slide 1: FORMATION OF NANOPHASE IN THE AMORPHOUS MATRIX OF THE Co77Si11B12 ALLOY DURING NON-ISOTHERMAL HEATING
Prepared by
Mariia Lopachak,
student of Faculty of Chemistry,
Ivan Franko National University of Lviv
Authors: Lopachak M.M., Boichyshyn L.M., Nosenko V.K.,
Hertsyk O.M., Kovbuz M.O.

## Slide 2
OBJECTS OF STUDY:
Co77Si11B12
Co-based amorphous metal alloys (AMA):
AIM OF STUDY:
The purpose of this work was to study the kinetics of the nanostructure of cobalt-based amorphous metal alloys.
METHODS:
differential scanning calorimetric (DSC) tests at three different heating rates (5 K/min, 10 K/min, 20 K/min)
X-ray diffraction analysis

## Slide 3
RESULTS OF THE DIFFERENTIAL SCANNING CALORIMETRY METHOD (DSC)
Figure 1: DSC curves of Co77Si11B12 at three different heating rates: 1 – 5 K/min; 2 – 10 K/min; 3 – 20 K/min.

## Slide 4
Sample | , К/хв | (Т2+Т1)/2, К | αІ | αІІ
Co77Si11B12 | 5 | 775 | 0,47 | 0,52
 | 10 | 787 | 0,51 | 0,42
 | 20 | 794 | 0,45 | 0,43
Fe80Si6B14 | 5 | 756 | 0,40 | 0,64
 | 10 | 769 | 0,42 | 0,51
 | 20 | 786 | 0,40 | 0,52
Fe84Nb2B14 | 5 | 689 | 0,56 | 0,68
 | 10 | 705 | 0,59 | 0,54
 | 20 | 709 | 0,54 | 0,56
Table 1. Change in the amount of crystalline phase (α) АМA at different heating rates of samples (, К/min) duringІ (αІ) and ІІ (αІІ) stage of crystalization.
Figure 2. The induction period of the І stage of the nanocrystallization process T` = T1–300 K (а) and the ІІ stage of complete crystallization T`` = T1`–T3 (b) АМA at different heating rates (, К/min).
RESULTS OF THE DIFFERENTIAL SCANNING CALORIMETRY METHOD (DSC)

## Slide 5
RESULTS OF THE DIFFERENTIAL SCANNING CALORIMETRY METHOD (DSC)
THERMODYNAMIC CHARACTERISTICS OF AMA`s NANOSTRUCTURE
Alloy |  | β, К/min | Т1, К | Ea1 , kJ/mol | Т2, К | Ea2 , kJ/mol | Т3, К | Ea3, kJ/mol
Co77Si11B12 | 1 peak | 5 | 761 | 347 | 776 | 374 | 788 | 266
 |  | 10 | 771 |  | 787 |  | 804 | 
 |  | 20 | 780 |  | 794 |  | 814 | 
 | 2 peak | 5 | 792 | 323 | 804 | 429 | 816 | 391
 |  | 10 | 804 |  | 814 |  | 829 | 
 |  | 20 | 814 |  | 821 |  | 834 | 
 | 3 peak | 5 | 816 | 327 | 819 | 314 | 827 | 338
 |  | 10 | 829 |  | 833 |  | 839 | 
 |  | 20 | 839 |  | 843 |  | 850 | 
Kissinger
kinetic model
  Figure 3. Kissinger`s dependencies of the first stage of AMA`s Co77Si11B12 nanocrystallization at temperatures:
1 - nucleation of the nanocrystalline phase;
2 - growth of the nanocrystalline phase;
3 - constant rate of nanocrystals formation.

## Slide 6: KINETIC PARAMETERS OF THE NANOSTRUCTURING PROCESS
Figure 4. The degree of crystallization (α) of AMA Co77Si11B12 as a function of temperature at three different heating rates (1 - 5 K / min; 2 - 10 K / min; 3 - 20 K / min).
ST - the total area of the exothermic peak
Si – the area between the starting point of the peak and the point at any other temperature within the peak.
The Matusita model[1]
where α is the volume fraction of nanocrystallization, β is the heating rate, Ea is the activation energy, n is the Avrami index, m is the growth dimension, R is the gas constant, T is the temperature, and C is the constant.
[1]Boichyshyn L. The Kinetic Peculiarities of the Nanocrystallization of Amorphous Alloys Fe84Nb2B14, which are Doped by Rare Earth Metals / L.Boichyshyn M.-O. Danyliak, B. Kotur, T. Mika // Physics and chemistry of solidstate V. 18, № 1 (2017) P. 122-128

## Slide 7
Alloy | T, К | n | b, К/min | m | p | b
Co77Si11B12 | 739 | 0,6 | 5 | 1,9 | 1 | -1,30<1
 |  |  | 10 | 2,9 | 0,5 | -0,85<1
 |  |  | 20 | 2,7 | 0,5 | -0,75<1
  KINETIC PARAMETERS ACCORDING TO THE MATUSITA MODEL OF NANOCRYSTALS GROWTH IN THE STRUCTURE OF ALLOYS UNDER THE INFLUENCE OF TEMPERATURE FOR THE DSC FIRST MAXIMUM.
Parameter | Value | Definition
m | 1 | The mechanism of 1-dimensional growth
 | 2 | The mechanism of 2-dimensional growth
 | 3 | The mechanism of 3-dimensional growth
p | 1 | Linear growth (interphase control)
 | 0.5 | Parabolic growth (diffusion control)
b | >1 | Increasing the nucleation rate
 | 0 | No nucleation in the crystallization process (all nuclei may be present before crystallization)
 | <1 | Reducing the nucleation rate

## Slide 8
Figure 5. Diffractograms of AMA Co77Si11B12 initial and annealed (± 5 K) at 719 (a) and 765 K with a heating rate of 5 K / min.
  STUDY OF AMORPHOUS ALLOYS BY X-RAY DIFFRACTION
а
b

## Slide 9: CONCLUSIONS
Based on the curve of heat release on heating, obtained by the differential scanning calorimetry (DSC), it is seen that in AMA Co77Si11B12 in the range of 700 - 900 K there are 3 structural transformations associated with the formation of clusters and crystalline phases.
The Matusita model was used to determine the kinetic parameters of the process of nanocrystals formation in the amorphous matrix of the investigated alloy.
According to the average value of the growth parameter m, it was determined that the AMA`s crystallization process of the Co-Si-B system depends on the heating rate and the nature of the alloying application.
The growth of Co nanocrystals in AMA Co77Si11B12 at heating rates of 10 and 20 K / min occurs at a 3-dimensional mechanism, and the value of p = 0.5 indicates diffusion-controlled crystallization.

## Slide 10: THANK YOU FOR YOUR ATTENTION!
If you have any questions, write to the e-mail:
lopachak1999mashka@gmail.com